ROTATIONAL CAPACITY TEST/RECORD

Wisconsin Department of Transportation

DT2113          9/2013

This form should be completed and filed with the as-built construction as a permanent record. One worksheet shall be completed for each rotational capacity lot number used on the project. A lot shall consist of any possible combination 
of nut and bolt to be used in the intended structure. This test is required prior to the start of bolt installation work on the project site.

| Region | Contract Number |
| --- | --- |
| Job Number | Project |
| Bolt Grade A325 A490 | Assigned R-C Lot Number |

Rotational Capacity Test Instructions (tables on back)

- Insert fastener assembly into a load cell(1) and tension according to Table 5.

- Match mark the nut and plate on the load cell, and turn until tension is at or above the Table 2.

- Record tension on Line 1.

- Record the torque on Line 2(2).

- Compare torque on Line 2 with Table 4 – torque should be less than the listed maximum when at tension on Line 1.

- Continue turning the nut, until reaching the total rotation of Table 1 and record the tension on Line 4.

- Compare tension on Line 4 with Table 3 and verify that it passed on Line 5.

- Loosen nut and examine assembly. Nuts should turn on by hand to the point tightened.

- Failure of any portion of the test in either of the two assemblies constitutes a failure of the test as listed below. When failure occurs, the subject lot of fasteners is rejected. The contractor is given the option to clean and re-lubricate as necessary and resubmit for testing

  - Exceeding maximum allowable torque/tension (Table 4).

  - Failure to achieve the required rotation (Table 1).

  - Failure to achieve the required tension at the required rotation (Table 3).

  - Thread failure – will not turn on by hand, shear cracks, stripping or torsional failures.

(1) For short bolts that won’t fit the load cell use a plate with a hole and skip the tension requirements.

(2) Measure torque while nut is turning.

|  | Bolt | Nut | Washer |
| --- | --- | --- | --- |
| Manufacturer |  |  |  |
| Lot Number |  |  |  |
| Diameter/Length | Inches |  |

| Rotational Capacity Test Record | Sample #1 | Sample #2 |
| --- | --- | --- |
| Measured tension at or above minimum in Table 2 | Kips | Kips |
| Measure torque after step 1 | Ft/Lbs | Ft/Lbs |
| Torque was less than maximum allowable from Table 4 | Pass Fail | Pass Fail |
| Measured tension* (after total rotation in Table 1) | Kips | Kips |
| Measured tension is above minimum allowable Table 3 | Pass Fail | Pass Fail |
| Verify thread condition | Pass Fail | Pass Fail |

*Applies to long bolts test only, leave blank for short bolts

| Tested By | Witnessed By |
| --- | --- |
| Location | Date (m/d/yyyy) |

See tables on back

| Table 1 Rotational-Capacity Test – Required Rotation(s) |
| --- |
| Bolt Length (L) Relative to Bold Diameter (D) | Rotation (Total) |
| L≤4D | 2/3 |
| L>4D/L≤8D | 1 |
| L>8D/L12D | 1 1/6 |
| Table 2 Minimum Measured Tension (Kips) |
| Bolt Dia. | 3/4" | 7/8" | 1" | 1 1/8" | 1 1/4" | 1 3/8" | 1 1/2" |
| A325 | 28 | 39 | 51 | 56 | 71 | 85 | 103 |
| A490 | 35 | 49 | 64 | 80 | 102 | 121 | 148 |
| Table 3 Measured Tension Minimum (Kips) at total rotation from Table 1 equals 1.15 × Table 2 |
| Bolt Dia. | 3/4" | 7/8" | 1" | 1 1/8" | 1 1/4" | 1 3/8" | 1 1/2" |
| A325 | 32 | 45 | 59 | 64 | 82 | 98 | 118 |
| A490 | 40 | 56 | 74 | 92 | 117 | 139 | 170 |
| Table 4 Rotational Capacity Maximum Torque |
| 3/4" Diameter | 7/8" Diameter | 1" Diameter | 1 1/8" Diameter | 1 1/4" Diameter | 1 3/8" Diameter | 1 1/2" Diameter |
| Kips Tension | Max. Torque | Kips Tension | Max. Torque | Kips Tension | Max. Torque | Kips Tension | Max. Torque | Kips Tension | Max. Torque | Kips Tension | Max. Torque | Kips Tension | Max. Torque |
| 28 | 441 | 39 | 712 | 51 | 1058 | 56 | 1316 | 71 | 1846 | 85 | 2444 | 103 | 3219 |
| 29 | 453 | 40 | 730 | 52 | 1079 | 57 | 1340 | 72 | 1872 | 86 | 2473 | 104 | 3250 |
| 30 | 469 | 41 | 748 | 53 | 1100 | 58 | 1363 | 73 | 1898 | 87 | 2501 | 105 | 3281 |
| 31 | 484 | 42 | 767 | 54 | 1121 | 59 | 1387 | 74 | 1924 | 88 | 2530 | 106 | 3313 |
| 32 | 500 | 43 | 785 | 55 | 1141 | 60 | 1410 | 75 | 1950 | 89 | 2559 | 107 | 3344 |
| 33 | 516 | 44 | 803 | 56 | 1162 | 61 | 1434 | 76 | 1976 | 90 | 2588 | 108 | 3375 |
| 34 | 531 | 45 | 821 | 57 | 1183 | 62 | 1457 | 77 | 2002 | 91 | 2616 | 109 | 3406 |
| 35 | 547 | 46 | 840 | 58 | 1204 | 63 | 1481 | 78 | 2028 | 92 | 2645 | 110 | 3438 |
| 36 | 563 | 47 | 858 | 59 | 1224 | 64 | 1504 | 79 | 2054 | 93 | 2674 | 111 | 3469 |
| 37 | 578 | 48 | 876 | 60 | 1245 | 65 | 1528 | 80 | 2080 | 94 | 2703 | 112 | 3500 |
| 38 | 594 | 49 | 894 | 61 | 1266 | 66 | 1551 | 81 | 2106 | 95 | 2731 | 113 | 3531 |
| 39 | 609 | 50 | 913 | 62 | 1287 | 67 | 1575 | 82 | 2132 | 96 | 2760 | 114 | 3563 |
| 40 | 625 | 51 | 931 | 63 | 1307 | 68 | 1598 | 83 | 2158 | 97 | 2789 | 115 | 3594 |
| 41 | 641 | 52 | 949 | 64 | 1328 | 69 | 1622 | 84 | 2184 | 98 | 2818 | 116 | 3625 |
| 42 | 656 | 53 | 967 | 65 | 1349 | 70 | 1645 | 85 | 2210 | 99 | 2846 | 117 | 3656 |
| 43 | 672 | 54 | 986 | 66 | 1370 | 71 | 1669 | 86 | 2236 | 100 | 2875 | 118 | 3688 |
| 44 | 688 | 55 | 1004 | 67 | 1390 | 72 | 1692 | 87 | 2262 | 101 | 2904 | 119 | 3719 |
| 45 | 703 | 56 | 1022 | 68 | 1411 | 73 | 1716 | 88 | 2288 | 102 | 2933 | 120 | 3750 |
| 46 | 719 | 57 | 1040 | 69 | 1432 | 74 | 1739 | 89 | 2314 | 103 | 2961 | 121 | 3781 |
| 47 | 734 | 58 | 1059 | 70 | 1453 | 75 | 1763 | 90 | 2340 | 104 | 2990 | 122 | 3813 |
| 48 | 750 | 59 | 1077 | 71 | 1473 | 76 | 1786 | 91 | 2366 | 105 | 3019 | 123 | 3844 |
| 49 | 766 | 60 | 1095 | 72 | 1494 | 77 | 1810 | 92 | 2392 | 106 | 3048 | 124 | 3875 |
| 50 | 781 | 61 | 1113 | 73 | 1515 | 78 | 1833 | 93 | 2418 | 107 | 3076 | 125 | 3906 |

| Table 5 Initial Tension +2 Kips –0 Kips |
| --- |
| Bolt Dia. | 3/4" | 7/8" | 1" | 1 1/8" | 1 1/4" | 1 3/8" | 1 1/2" |
| A325 | 3 Kips | 4 Kips | 5 Kips | 6 Kips | 7 Kips | 9 Kips | 10 Kips |
| A490 | 4 Kips | 5 Kips | 6 Kips | 8 Kips | 10 Kips | 12 kips | 15 Kips |